Porcelain Veneer Insertion

Patient:			 Date

Remove Provisional’s

Remove Spot Bonding

Chlorahexidine rinse and scrub

Floss and Ceri Strip contacts

Pumice with soft rubber cup and gravy

Shade Verification with try in Jelly

Rubber Dam slot technique

Dry Try in all restorations

Silane Porcelain lightly air dry

Etch Enamel and dentin

Gluma thoroughly on all dentin surfaces

Adhesive on Porcelain

Primer and Adhesive 4th generation

Veneer cement – 3m rely x

Rapid seat starting at midline

Clean 80% of cement on facial margins

Tack for 3-5 seconds at gingival margin

Clean lingual and interproximal cement with camel hair brush

Glycerin, Light cure 40 seconds each

12 Blade at margins and interporx

Ceri strip and diamond strips

Floss and re clean as needed

Football bur on lingual

Check occlusion

Polish margins

Patient Instructions

Doctor:

Assistant :